ALUMINIUM

REACH

##### CONSORTIUM

Joint  initiative  of  EAA  (European Aluminium Association)

and  IAI  (International Aluminium Institute)

Substance Identity Profile (SIP) and analytical methods.

Identification:

Substance name: 			Aluminium oxide

IUPAC name:			dialuminum; oxygen(2-)

Other trade names:		Alumina, Fused alumina , Activated alumina, Smelter grade alumina

Molecular formula:			Al2O3

Molar mass:			101,96

CAS No.:			1344-28-1

EINECS No.:			215-691-6

Substance definition:

The substance to be registered is Aluminium oxide as a mono-constituent substance.

Composition:

| Parameter | CAS No. | EC No. | Name | Concentration Range | Concentration Typical |
| --- | --- | --- | --- | --- | --- |
| Constituent | 1344-28-1 | 215-691-6 | Aluminium oxide | > 95% | 99,7 |
| Impurities | 1313-59-3 | 215-208-9 | Sodium oxide | > 0,05 to < 2,6% | 0,25 |
|  | 7631-86-9 | 231-545-4 | Silica | > 0,005 to < 0,4% | 0,01 |
|  | 1305-78-8 | 215-138-9 | Calcium oxide | > 0,005 to <0,4% | 0,01 |
|  | 1345-25-1 | 215-721-8 | Iron oxide | > 0,01 to <1,5% | 0,01 |
|  |  |  | Other | 0,0001 to <0,1 | <0,02 |

Technological process:

Aluminium oxide is produced from calcination of aluminium hydroxide

Classification & Labelling:

Aluminium oxide is not classified under Regulation (EC) 1272/2008.

Recommendation for analytical methods for substance identification and determination of composition/purity:

- Identify the substance by XRD (X-Ray diffraction)

- Determine composition by XRF (X-Ray Fluorescence)